IPC 4761

Abstract

| Type | Description | Covering-Material |
| --- | --- | --- |
| I-a / -b | Tented one-sided / double-sided | Dryfilm solder-stop |
| II-a / -b | Tented & Covered one-sided / double-sided | Dryfilm solder-stop + LPI solder-stop |
| III-a / -b | Plugged one-sided / double-sided | Plugging Epoxy (non-conducting paste) |
| IV-a / -b | Plugged & Covered one-sided / double-sided | Plugging Epoxy + LPI solder-stop |
| V | Filled | Plugging Epoxy (non-conducting paste) |
| VI-a / -b | Filled & Covered one-sided / double-sided | Plugging Epoxy + LPI solder-stop |
| VII | Filled & Capped | Special Plugging Epoxy + plating |

A.Via Tenting

IPC 4761 Type I: Tented Via

The via is completely covered with  dryfilm solder-stop.
One-sided: Type I-a
Double-sided:Type I-b

IPC 4761 Type II: Tented & Covered Via

The via is completely covered with  dryfilm solder-stop

and overprinted with normal solder-stop, afterwards.
One-sided: Type II-a
Double-sided:Type II-b

### Application

- Protection of solder floating up to the component side

- Enables vacuum-adaption for production

- Covering of critical vias, e.g. beneath BGA

### Alternatives

You can apply Via Filling, alternatively.

Through cutting the solder-stop clearance, you can ensure a sufficient solder-stop bridge for BGAs. Using this method, the via annular rings will be partly covered with solder-stop.

### Parameters

| Covering | Max. Drill-Ø |
| --- | --- |
| Via Tenting | 300µm |

B.Via Plugging

IPC 4761 Type III: Plugged Via
The via is partially filled with non-conductive paste.
One-sided: Type III-a
Double-sided: Type III-b

IPC 4761 Type IV: Plugged & Covered Via

The via is partially filled with non-conductive paste and

overprinted with normal solder-stop, afterwards.
One-sided: Type IV-a
Double-sided: Type IV-b
It is recommended as one-sided plugging (Type III-a / Type IV-a)

as there is a chance of cracks through encapsulated gas while

soldering double-sided plugged vias.
Application

- Protection of solder floating up to the component side

- Enables vacuum-adaption for production

| ParametersCovering | Min. Drill-Ø | Max. Drill-Ø |
| --- | --- | --- |
| Via Filling | 250µm | 500µm |

C. Via Filling

IPC 4761 Type V: Filled Via

The via is filled completely with non-conductive paste.

IPC 4761 Type VI: Filled & Covered Via

The via is filled completely with non-conductive paste

and overprinted with normal solder-stop, afterwards.

One-sided: Type VI-a
Double-sided: Type VI-b

IPC 4761 Type VII: Filled & Capped Via

The via is plated-through and cleaned - afterwards a

non-conductive paste is forced in and hardened - the ends

are planarized, metallized and plated-over. Hence,

the surface is planar and solderable.

This technology is mostly used for Via in Pad solutions and is also applied for stacked und staggered (Micro-)vias. Via Plugging faciliates routing of additional conductor traces between BGA vias amongst other things.